Single skin pierced fixed cladding (Galvalume Sheets-Colour) Enquiry Item. 01  Matl code:HY7810278045

Specification:

Supply of colour coated galvalume hirib profile sheet of nominal 1015-1020 mm effective cover width and 28-30 mm deep ribs with subtle square fluting in the five pan at nominal 202-205 mm centre-to-centre. The end rib shall be designed for anti-capillary action, to avoid any seepage of water through the lateral overlap. The feed material is manufactured out of nominal 0.45 mm Base Metal Thickness (BMT) or 0.5mm TCT, Hi-strength steel with minimum 550 MPa yield strength, metallic hot dip coated with Aluminium-Zinc alloy (55% Aluminium, 45% Zinc) as per AS 1397 –Zincalume AZ150 (Min. 150 gms/sq.mt total on both sides) with colourbond steel quality paint coat as per AS/NZS 2728 type 3-4. The paint shall have a total coating thickness of nominal 35 μm, comprising of nominal 20 μm exterior coat on top surface and nominal 5 μm reverse coat on back surface over nominal 5 μm primer coat on both surfaces of approved colour shade by concern authority. The steel manufacturer’s test certificate for the chemical and mechanical properties of steel must be submitted for approval by the engineer-in-charge.

Unit:

Square Metre

Single skin pierced fixed cladding (Galvalume Sheets-Bare) Enquiry Item. 02  Matl code:HY7810278053

Specification:

Supply of non - colour coated galvalume  hirib profile sheet of nominal 1015-1020 mm effective cover width and 28-30 mm deep ribs with subtle square fluting in the five pan at nominal 202-205 mm centre-to-centre. The end rib shall be designed for anti-capillary action, to avoid any seepage of water through the lateral overlap. The feed material is manufactured out of nominal 0.45 mm Base Metal Thickness (BMT) or 0.5mm TCT, Hi-strength steel with minimum 550 MPa yield strength, metallic hot dip coated with Aluminium-Zinc alloy (55% Aluminium, 45% Zinc) as per AS 1397 –Zincalume AZ150 (Min. 150 gms/sq.mt total on both sides). The steel manufacturer’s test certificate for the chemical and mechanical properties of steel must be submitted for approval by the engineer-in-charge.

Unit:

Square Metre

Plain Barge Boards  Enquiry Item. 03  Matl code:HY7810278061

Specification:

Supply of colour coated 200 mm size galvalume plain barge boards of nominal 0.45 mm Base Metal Thickness (BMT) or 0.5mm TCT, Hi-strength steel with minimum 550 MPa yield strength, metallic hot dip coated with Aluminium-Zinc alloy (55% Aluminium, 45% Zinc) as per AS 1397 –Zincalume AZ150 (Min. 150 gms/sq.mt total on both sides) with colourbond steel quality paint coat as per AS/NZS 2728 type 3-4. The paint shall have a total coating thickness of nominal 35 μm, comprising of nominal 20 μm exterior coat on top surface and nominal 5 μm reverse coat on back surface over nominal 5 μm primer coat on both surfaces of colour shade same as galvalume cladding. The steel manufacturer’s test certificate for the chemical and mechanical properties of steel must be submitted for approval by the engineer-in-charge.

Unit:

Running Metre

Flashing Hood  Enquiry Item. 04  Matl code:HY7810278070

Specification:

Supply of colour coated galvalume plain sheet for flashing hood (gable, corner etc.) of nominal 0.45 mm Base Metal Thickness (BMT) or 0.5mm TCT, Hi-strength steel with minimum 550 MPa yield strength, metallic hot dip coated with Aluminium-Zinc alloy (55% Aluminium, 45% Zinc) as per AS 1397 –Zincalume AZ150 (Min. 150 gms/sq.mt total on both sides) with colourbond steel quality paint coat as per AS/NZS 2728 type 3-4. The paint shall have a total coating thickness of nominal 35 μm, comprising of nominal 20 μm exterior coat on top surface and nominal 5 μm reverse coat on back surface over nominal 5 μm primer coat on both surfaces of colour shade same as galvalume cladding. The steel manufacturer’s test certificate for the chemical and mechanical properties of steel must be submitted for approval by the engineer-in-charge.

Unit:

Square Metre

North Light Curves Enquiry Item. 05  Matl code:HY7810278088

Specification:

Supply of North Light curves made of colour coated galvalume hirib profile sheet of nominal 1015-1020 mm effective cover width and 28-30 mm deep ribs with subtle square fluting in the five pan at nominal 202-205 mm centre-to-centre. The North light curve cross-sectional profile is of 882.5 mm length consisting of circular curve of 537.5 mm length, 425.8 mm radius and straight line profile of 345 mm length. The end rib shall be designed for anti-capillary action, to avoid any seepage of water through the lateral overlap. The feed material is manufactured out of nominal 0.45 mm Base Metal Thickness (BMT) or 0.5mm TCT, Hi-strength steel with minimum 550 MPa yield strength, metallic hot dip coated with Aluminium-Zinc alloy (55% Aluminium, 45% Zinc) as per AS 1397 –Zincalume AZ150 (Min. 150 gms/sq.mt total on both sides) with colourbond steel quality paint coat as per AS/NZS 2728 type 3-4. The paint shall have a total coating thickness of nominal 35 μm, comprising of nominal 20 μm exterior coat on top surface and nominal 5 μm reverse coat on back surface over nominal 5 μm primer coat on both surfaces of approved colour shade by concern authority. The steel manufacturer’s test certificate for the chemical and mechanical properties of steel must be submitted for approval by the engineer-in-charge.

Unit:

Running Metre