BHEL JHANSI

Specification of Men’s Uniform Cloth (Pant)

Ref: BHEL/JHS/HR/WLF/uniform/02

- Scope of the specification covers the requirement of uniform (pant) cloth for men.

- Sample of Uniform Cloth

The vendor will submit sample and conformance certificate as per specification No: BHEL/JHS/HR/WLF/uniform/02 along with their quotation. Maximum three samples can be submitted with offer by each bidder. Each sample should be at least 50X50 cm piece of cloth and shall have name and signature of the bidder and tender enquiry no.

- Test Certificate: Test certificate shall be submitted along with bulk supply after carrying out test as per the technical parameters mentioned in point 7 on each lot of supply against BHEL order.

- Packing & Marking: Each piece of cloth should be packed in a polythene bag. Blend composition and name of the manufacturer will be printed on the cloth.

- Inspection of the cloth: Final inspection will also be carried out at our works with reference to the approved sample and BHEL/JHS/HR/WLF/Uniform/02/2010  and test report submitted along with supply and as per purchase order. BHEL Jhansi may inspect at manufacturer’s work at its discretion with reference to the approved sample and technical parameters with reference to BHEL/JHS/HR/WLF/Uniform/02/2010. The supplier shall give inspection call before dispatch of cloth.

- Qualification of the vendor: The vendor should be original cloth manufacturer and must have executed order of minimum Rs. 3 lakh in last three years to Govt./PSU/private organizations.

Page 01

| 1. 2. 3. 4. 5 6 7 8 9 10 11 12 13 14 15 16 17 | Colour of cloth Blend Composition (Polyster:Cotton) Cut Length Width Yarn Number - NE - Warp Weft Thread Density Per Inch. - Ends Picks Weight Per Sq - Mtr - Grams Breaking Strength - KGF 20 x 5 Cms Ravel led Strip - Warp Crease Recovery Angle - Degrees Warp + Weft Shrinkage When Heated - Warp - Weft Relaxation Shrinkage - Warp - Weft Ph of Aqueous Extract. Water Soluble Colour Fasteness Test a) Lighting - Class b) Washing - Change in Colour - Staining on Undyed Piece c) Perspiration Acidic - Change in Colour - Straining on Undyed Piece Alkaline - Change in Colour - Staining on Undyed Piece Fibre Composition - Warp P/C - Weft P/C Rubbing (Pilling) Weave | Smoke Grey 80/20 +/-5% 1.2 to 1.5 meter 150 Cms +/-1 Cm 2/30s +/-5% 30 DN Tex 92 +/-5% 64 +/-5% 245.0 +/-5% 130 (Min) 115 (Min) 240 (Min) 2.0 Max 2.0 Max 1.0 Max 1.0 Max 6-9.5 1% Maximum 4 or better 4 or better 4 or better 4 or better 4 or better 4 or better 4 or better 67/33 +/-2% 100 Polyester 4 or better Gabardine |
| --- | --- | --- |

7. Technical parameters with reference to IS: 15853/2009 for Pant cloth

Page 02

BHEL JHANSI

Specification of Men’s Uniform Cloth (Shirt)

Ref: BHEL/JHS/HR/WLF/uniform/01

- Scope of the specification covers the requirement of uniform (shirt) cloth for men.

- Sample of Uniform Cloth

The vendor will submit sample and conformance certificate as per specification No: BHEL/JHS/HR/WLF/uniform/01 along with their quotation. Maximum three samples can be submitted with offer by each bidder. Each sample should be at least 50X 50 cm piece of cloth and shall have name and signature of the bidder and tender enquiry no.

- Test Certificate: Test certificate shall be submitted along with bulk supply after carrying out test as per the technical parameters mentioned in point no. 7 on each lot of supply against BHEL order.

- Packing & Marking: Each piece of cloth should be packed in a polythene bag. Blend composition and name of the manufacturer will be printed on the cloth.

- Inspection of the cloth: Final inspection will also be carried out at our works with reference to the approved sample and BHEL/JHS/HR/WLF/Uniform/01/2010  and test report submitted along with supply and as per purchase order. BHEL Jhansi may inspect at manufacturer’s work at its discretion with reference to the approved sample and technical parameters with reference to BHEL/JHS/HR/WLF/Uniform/01/2010. The supplier shall give inspection call before dispatch of cloth.

- Qualification of the vendor: The vendor should be original cloth manufacturer and must have executed order of minimum Rs. 3 lakh in last three years to Govt./PSU/private organizations.

Page 01

7. Technical parameters with reference IS: 15852/2009 for shirt cloth

| 1. 2. 3. 4. 5. 6. 7. 8. 9. 10. 11. 12. 13. 14. 15. | Technical Parameters Colour of Cloth Blend Composition Cut Length Width Yarn Number - NE - Warp Weft Thread Density Per Inch. - Ends Picks Weight Per Sq - Mtr - Grams Breaking Strength - KGF 20 x 5 Cms Ravel led Strip - Warp Shrinkage When Heated % - Warp - Weft Relaxation Shrinkage % - Warp - Weft Ph of Aqueous Extract. Water Soluble Colour Fasteness Test a) Lighting - Class b) Washing - Change in Colour - Staining on Undyed Piece c) Perspiration Acidic - Change in Colour - Straining on Undyed Piece Alkaline - Change in Colour - Staining on Undyed Piece Fibre Composition - Warp P/C - Weft P/C Rubbing (Pilling) Weave | Smoke Grey 67 % /33 +/-2% 2.20-2.50 meter 90 Cms +/-1 Cm 2/80s PC +/-5% 2/80s PC +/-5% 140 +/-5% 80 +/-5% 140.0 +/-5% 80 Kgf (Min) 45 Kgf (Min) 2.0 Max 2.0 Max 1.0 Max 1.0 Max 6 -9.5 1% Maximum 4 or better 4 or better 4 or better 4 or better 4 or better 4 or better 4 or better 67/33 +/-2% 67/33 +/-2% 4 or better Plain |
| --- | --- | --- |

Page 02

BHEL JHANSI

Requirements for Saree/blouse/petticoat

- Scope of the specification covers the requirement of saree, blouse and petticoat.

- Sample of Uniform Cloth

The vendor will submit sample along with their quotation. Maximum three samples can be submitted with offer by each bidder. Each sample should be at least 50X50 cm piece of cloth and shall have name and signature of the bidder and tender enquiry no.

- Packing & Marking: Each piece of cloth should be packed in a polythene bag. Blend composition and name of the manufacturer will be printed on the cloth.

- Inspection of the cloth: Final inspection will also be carried out at our works with reference to the approved sample and test report submitted along with supply and as per purchase order. BHEL Jhansi may inspect at manufacturer’s work at its discretion with reference to the approved sample. The supplier shall give inspection call before dispatch of cloth.

- Qualification of the vendor: The vendor should be original cloth manufacturer and must have executed order of minimum Rs. 3 lakh in last three years to Govt./PSU/private organizations.