Annexure-I

SPECIFICATION FOR FIBRE CORE STEEL WIRE ROPE

SIZE-13 MM

| Description | Specification | Supplier Confirmation | Remarks |
| --- | --- | --- | --- |
| Size of wire | 13 mm |  |  |
| Steel wire | Un-Galvanized |  |  |
| Type of wire | Bright Round wire as per IS:1835. |  |  |
| Construction | 6x36 (14-7+7-7-1) |  |  |
| Core | Natural Fibre |  |  |
| Turn (Direction) | RHO |  |  |
| Min. Tensile Strength, Tensile Strength test as per IS:1608 (Superseding IS:1521) | 1770 N/MM2, Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Min. Breaking load as per IS:2266, Breaking Load Test as per IS:6594 | 99 KN, Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Bending Test as per IS:1716 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Torsion Test as per IS:1717 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Chemical composition as per relevant part of steel wire rope of IS:228 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. Chemical composition may be rechecked by BHEL at BHEL Bhopal before final acceptance. |  |  |
| Testing Confirmation As Per Indian Standard | IS:2266-2002 |  |  |
| Witness of tests | Minimum following tests such as Tensile strength, Breaking Load, Bending test, Torsion test will be witnessed by BHEL, Bhopal representative at manufacturer’s work. |  |  |
| Roll Size (Max.) | 1000 Mtr/Roll |  |  |

Note :- Only latest revision of all IS to be followed.

Annexure-II

SPECIFICATION FOR FIBRE CORE STEEL WIRE ROPE

SIZE-18 MM

| Description | Specification | Supplier Confirmation | Remarks |
| --- | --- | --- | --- |
| Size of wire | 18 mm |  |  |
| Steel wire | Un-Galvanized |  |  |
| Type of wire | Bright Round wire as per IS:1835. |  |  |
| Construction | 6x36 (14-7+7-7-1) |  |  |
| Core | Natural Fibre |  |  |
| Turn (Direction) | RHO |  |  |
| Min. Tensile Strength, Tensile Strength test as per IS:1608 (Superseding IS:1521) | 1770 N/MM2, Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Min. Breaking load as per IS:2266, Breaking Load Test as per IS:6594 | 189 KN, Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Bending Test as per IS:1716 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Torsion Test as per IS:1717 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Chemical composition as per relevant part of steel wire rope of IS:228 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. Chemical composition may be rechecked by BHEL at BHEL Bhopal before final acceptance. |  |  |
| Testing Confirmation As Per Indian Standard | IS:2266-2002 |  |  |
| Witness of tests | Minimum following tests such as Tensile strength, Breaking Load, Bending test, Torsion test will be witnessed by BHEL, Bhopal representative at manufacturer’s work. |  |  |
| Roll Size (Max.) | 1000 Mtr/Roll |  |  |

Note :- Only latest revision of all IS to be followed.

Annexure-III

SPECIFICATION FOR FIBRE CORE STEEL WIRE ROPE

SIZE-26 MM

| Description | Specification | Supplier Confirmation | Remarks |
| --- | --- | --- | --- |
| Size of wire | 26 mm |  |  |
| Steel wire | Un-Galvanized |  |  |
| Type of wire | Bright Round wire as per IS:1835. |  |  |
| Construction | 6x36 (14-7+7-7-1) |  |  |
| Core | Natural Fibre |  |  |
| Turn (Direction) | RHO |  |  |
| Min. Tensile Strength, Tensile Strength test as per IS:1608 (Superseding IS:1521) | 1770 N/MM2, Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Min. Breaking load as per IS:2266, Breaking Load Test as per IS:6594 | 395 KN, Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Bending Test as per IS:1716 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Torsion Test as per IS:1717 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Chemical composition as per relevant part of steel wire rope of IS:228 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. Chemical composition may be rechecked by BHEL at BHEL Bhopal before final acceptance. |  |  |
| Testing Confirmation As Per Indian Standard | IS:2266-2002 |  |  |
| Witness of tests | Minimum following tests such as Tensile strength, Breaking Load, Bending test, Torsion test will be witnessed by BHEL, Bhopal representative at manufacturer’s work. |  |  |
| Roll Size (Max.) | 500 Mtr/Roll |  |  |

Note :- Only latest revision of all IS to be followed.

Annexure-IV

SPECIFICATION FOR FIBRE CORE STEEL WIRE ROPE

SIZE-32 MM

| Description | Specification | Supplier Confirmation | Remarks |
| --- | --- | --- | --- |
| Size of wire | 32 mm |  |  |
| Steel wire | Un-Galvanized |  |  |
| Type of wire | Bright Round wire as per IS:1835. |  |  |
| Construction | 6x36 (14-7+7-7-1) |  |  |
| Core | Natural Fibre |  |  |
| Turn (Direction) | RHO |  |  |
| Min. Tensile Strength, Tensile Strength test as per IS:1608 (Superseding IS:1521) | 1770 N/MM2, Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Min. Breaking load as per IS:2266, Breaking Load Test as per IS:6594 | 598 KN, Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Bending Test as per IS:1716 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Torsion Test as per IS:1717 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. |  |  |
| Chemical composition as per relevant part of steel wire rope of IS:228 | Confirmation for providing Test Certificate from manufacturer of wire during on-site inspection of wire rope and also along with supply of item. Chemical composition may be rechecked by BHEL at BHEL Bhopal before final acceptance. |  |  |
| Testing Confirmation As Per Indian Standard | IS:2266-2002 |  |  |
| Witness of tests | Minimum following tests such as Tensile strength, Breaking Load, Bending test, Torsion test will be witnessed by BHEL, Bhopal representative at manufacturer’s work. |  |  |
| Roll Size (Max.) | 500 Mtr/Roll |  |  |

Note :- Only latest revision of all IS to be followed.